COTTON FIBERS

Since 1915, CLAREMONT FLOCK has been providing high quality and consistency in short cut technical

fibers worldwide.  Our technical leaders have decades of combined experience to develop a complete custom designed solution or provide an existing one to satisfy any fiber need.

Our technical fibers are currently used in a variety of products to improve various performance properties such as: flexibility, reinforcement, tensile strength, security, identification, durability, texture, etc.  Let us assist you in making a superior product.  The information below reflects this expertise and we hope you consider us your short fiber solution partner.

AVAILABLE PRODUCT FORMS

Fiber type: RANDOM SIZED COTTON FIBER

Size (diameter):				10 µ - 15 µ (Microns)

Fineness (in Denier):			1.3 - 2.0 (OTHERS UPON REQUEST)

Cross section:				Variable:  Generally Round or Oval, often Irregular

Length (Specification):			80% between 0.37 mm (0.015") to 1.25 mm (0.050")

Dispersion in water:

At Room temp:			Even distribution

At Boiling:				Even distribution

Moisture Regain:				6% to 8% (70°F 60% RH)

General:					Good abrasion resistance; Attacked by mildew; Good

adhesion to natural and synthetic rubber compounds

Degrades in hot acids. Excellent resistance to alkali.

TECHNICAL PROPERTIES

Specific Gravity:				1.5 g/cm³

Melting Point:				Does not melt.

Temperature Effects:			Decomposes between 185°C (365°F) and 205°C (401°F)

Yellows at 120°C (248°F)

Chemical Reactivity:

Resistance to Acids:		Good

Resistance to Weak Alkali:		Excellent

Resistance to Solvents: 			Good

Resistance to Aging: 			Excellent

Resistance to Mildew:			Weak

Resistance to Sunlight:			Prolonged exposure causes loss of strength and yellowing.

TYPICAL APPLICATION

Apparel, Packaging, Wall Coverings, Cosmetics, Drapery Backing, Latex Glove Lining, Filler / Strengthening Agent for Rubber Compounds, Flocking, Security Enhancements for Papers and Plastics, Colorant for Paper & Plastic, Construction Joint Tape, Strengthening Agent for Epoxies, Medical Applications.